HEALTHCARE FACILITIES GUIDE

PAINTING SPECIFICATIONS

09 91 13 Exterior Painting

09 91 23 Interior Painting

November 15, 2022

Finish Coats, Sealers and Primers …………………………………………………………………………………………………………….3-4

Surface Preparation	5

Project Conditions for Painting Exterior Surfaces	5

INTERIOR PAINT SYSTEMS:

Admissions	6-8

Reception, Waiting Areas, Lobbies, Common Areas	8-9

Offices, Conference Rooms, Multi-Purpose Rooms	10-13

Hallways, Corridors, Common Areas	11-13

Nurses Stations, Administrative Center	13-15

Examination, Consulting and Treatment Rooms	15-17

Medical/Clinical Pathology and Laboratories, LABS	17-19

Imaging / Radiology	19-21

Patient Rooms	21-24

Labor and Delivery, Recovery and Maternity Suites	24-26

Nursery	26-28

Emergency Room, ER or ED	28-30

Intensive Care Unit, ICU, SICU, SUBICU	30-32

Neonatal Intensive Care Unit, NICU	32-34

Operating Rooms, OR, Surgical Suites, Medical/Surgical Units, Med Surg Unit	34-36

Patient Recovery Rooms, Post OP	36-38

Patient Rehabilitation and Therapy Rooms	38-40

Pharmacy	40-41

Kitchen, Food Preparation and Food Services	42-44

Cafeteria, Restaurants and Café	44-46

Medical Staff Lounge, Breakrooms, Storage Lockers, Toilet Rooms	46-48

Linen and Laundry Services	48-49

Central Sterile Services, CSSD	50-52

Central Supply Room	52-53

Janitorial Office, Break Room, and Common Space	54-55

Custodian Rooms, Janitorial Closets, Storage and Utility Rooms	55-57

Public Restrooms	57-59

Engineering and Facilities Offices, Storage Rooms, and Common Areas	60

Wood, Interior Stained and Transparent Finishes……………………………………………………………………………………………..61

Wood, Interior Clear Transparent Finishes………………………………………………………………………………………………… ….61

Concrete Floors, Painted, Pedestrian Traffic…………………………………………………………………………………………………..61

Concrete Floors, Painted, Heavy Traffic………………………………………………………………………………………………………. 61

## EXTERIOR PAINT SYSTEMS:

Concrete	61

Stucco and Cement Plaster	62

Fiber Cement - Pre-Primed…………………………………………………………………………………………………………………..	62

Concrete Masonry Units (CMU)……………………………………………………………………………………………………………...62-63

Concrete, Unfinished Decks, Stone, and Brick	63

Wood: Painted	63

Wood: Stained	63

Wood: Exterior Transparent Finishes……………..…………………………………………………………………………………………….63

Ferrous Metal: Steel and Wrought Iron	63

Non-Ferrous Metal: Galvanized Metal, and Brass	63

Aluminum…………………………………………………………………………………………………………………………………………...63

# BEHR® PAINT PRODUCTS

The Painting Schedule outlined in this guide is not all inclusive of available Behr® Paint and Kilz® products. Architects and specifiers may adapt and make changes, which are suitable for specific commercial projects and their requirements.

BEHR® and KILZ® Coatings in this guide comply with established local, state, and E.P.A. VOC content regulations, including South Coast Air Quality Management District (SCAQMD) Rule 1113. Behr® Paints help projects earn LEED® v4.1 credits, and are Master Painters Institute® (MPI) listed and approved, which meet MPI Green Performance® Standards.

## FINISH COATS

BEHR® COPPER FORCE™ Interior Paints are EPA-registered virucidal and antibacterial paints. This 100% acrylic paint & primer kills 99.9% of viruses [SARS-CoV-2 and Feline calicivirus (EPA proxy for Human Noroviruses)] and bacteria [Staphylococcus aureus (Staph) and Pseudomonas aeruginosa] within two hours of contact on the painted surface and lasts for up to six years. EPA Reg. No. 32273-10. It maintains its virucidal and anti-bacterial performance after repeated washings and contamination. Eggshell and Semi-Gloss finishes are available for gypsum board, concrete, masonry, wood, metal, and plastic substrates.

BEHR ULTRA™ SCUFF DEFENSE™ Interior Paints set a new standard for flat paint durability. SCUFF DEFENSE™ Stain-Blocking Paint & Primer in One featuring breakthrough innovation to deliver superior scuff and burnish resistance that are truly durable for high-traffic areas. Available in Flat, Eggshell, Satin and Semi-Gloss finishes.

BEHR PREMIUM PLUS® Interior Paints are a line of premium interior paints that provide durable and washable finishes. They also have low odor, and excellent touch-up properties. Available in Flat, Eggshell Satin, Semi-Gloss and Hi-Gloss sheens.

BEHR PRO® i300 Series Interior Paints are a top-line professional quality latex paints, which provide superior hide and coverage, excellent sprayability, and superior touch-up. Available in Flat, Eggshell and Semi-Gloss finishes.

BEHR PRO® Pre-Catalyzed Waterborne Epoxy is a single-component acrylic epoxy coating designed for interior and exterior use in USDA inspected commercial, institutional, and industrial facilities. This product provides exceptional adhesion as well as resistance to abrasion, stains, and most chemicals making it ideal for high maintenance areas subject to frequent cleaning. Available in Eggshell and Semi-Gloss sheens.

BEHR PREMIUM® Interior/Exterior Direct-To-Metal Paint is engineered for excellent corrosions resistance and adhesion to a variety  of properly prepared or primed residential and light industrial metal surfaces. It provides a durable finish that withstands tough elements on both interior and exterior surfaces. Use on other properly prepared and primed drywall, wood, and masonry. Available in Eggshell, Semi-Gloss, and Gloss sheens.

BEHR PREMIUM® Porch & Patio Floor Paint is an interior/exterior latex paint designed to provide a durable, mildew-resistant finish that resists scuffing, fading, cracking, and peeling for horizontal applications. Available in Low Lustre and Gloss sheens.

BEHR PREMIUM® Porch & Patio Anti-Slip Floor Paint is a 100% acrylic textured low-lustre enamel that is ideal for interior/exterior applications on wood and concrete porches, patios, pool decks and walkways to provide a durable, mildew-resistant finish that resists scuffing, fading, cracking, and peeling for horizontal applications.

BEHR PREMIUM PLUS® Exterior Paints are a line of premium exterior paints that provides a mildew-resistant finish with excellent durability and hide. It resists moisture, fading, and staining. Available in Flat, Satin, Semi-Gloss and Gloss sheens.

BEHR PRO®e600 Series Exterior Paints are a top-line, professional quality exterior paints that provide superior hide and coverage, excellent sprayability, and superior touch-up. Available in Flat, Satin® and Semi-Gloss sheens.

BEHR PREMIUM® Exterior High Build Coating is formulated as a self-priming coating over concrete and masonry surfaces. It is a flexible, long-lasting smooth waterproofing coating that withstands wind-driven rain up to 98 mph and may be applied directly to “HOT” masonry surfaces with pH levels up to 13. This coating also provides a breathable film that has up to 350% elongation.

BEHR PRO® Exterior Acrylic Texture Coating - Medium is specifically designed to provide a textured flat finish on properly prepared interior and exterior above-grade surfaces. This product minimizes defects and irregularities found on concrete and masonry surfaces. It provides a mildew resistant finish on the paint film. Performance data confirms its Resistance to Wind-Driven Rain (ASTM D6904). Not for use on horizontal surfaces (floors, roofs, decks.

BEHR PREMIUM® Protector & Waterproofer is an interior/exterior water-based waterproofer formulated with silicone to penetrate into the surface to help keep water out and shield against salt damage and corrosion. This product also reduces staining caused by mold and mildew and ensures greater durability of the surface.

BEHR PREMIUM® Semi-Transparent Waterproofing Stain & Sealer is a 100% acrylic formula that seals out the elements, and sun’s harmful UV rays, for decks, fences & siding. It is available in a curated collection of 60 color choices designed to help create a look that is as beautiful as it is durable.

BEHR PREMIUM® Solid Color Waterproofing Stain & Sealer is a 100% acrylic formula that seals out the elements, and sun’s harmful UV rays, for decks, fences, and siding. It forms an exceptionally durable and mildew-resistant finish that resists scuffing, cracking, peeling, and blistering.

BEHR® Fast-Drying Water-Based Wood Stain is designed for easy application and workability to interior wood surfaces such as cabinets, trim, doors, paneling, furniture and floors. This product provides superior color control, one-coat coverage and lower odor than oil-based stains.

BEHR® Fast-Drying Water-Based Polyurethane is designed to provide a crystal clear, self-leveling smooth finish that protects and beautifies interior wood. This product has less odor than oil-based finishes and resists stains and scratches. Ideal for bare or stained furniture, molding, cabinets, trim and wood doors. Available in matte, satin, semi-gloss and gloss sheens.

BEHR® Water-Based Spar Urethane is designed to provide a durable clear protective finish for exterior and interior wood surfaces. This finish is fortified with UV inhibitors for wood exposed to direct sunlight such as handrails and doors.

MONOCHEM PERMASHIELD® 200* is an advanced two-component water-based, aliphatic polyurethane that exhibits outstanding film hardness and excellent resistance against abrasion, chemicals, stains, direct/ reverse impacts, and ultraviolet light. When applied with a full broadcast of silica sand #30 over concrete, the coating provides a coefficient of friction (ASTM C1028) of 0.76 (wet) and 0.89 (dry). It is low odor and low VOC. Available in matte and high gloss, and in clear or colors.

*MONOPOLE, Inc., MONOCHEM PERMASHIELD 200 is not manufactured by Behr Paint Company. It is offered as an outsourced product in the BEHR PRO® third-party product program. Behr Paint Company is an authorized Distributor for Monopole, Inc., Los Angeles, California.

## PRIMERS AND SEALERS

BEHR® Drywall Plus Interior Primer & Sealer, 73 is fast-drying and seals uncoated and previously painted interior drywall, wallboard, plaster, wood and brick to promote a uniform finish for topcoats. This 100% acrylic, low VOC formula is ideal for use under lower sheen paints and has excellent hiding properties for topcoat products.

BEHR® Kitchen, Bath & Trim Interior Stain-Blocking Primer & Sealer, 75  promotes excellent adhesion to glossy surfaces and provides maximum stain resistance in a multi-purpose stain-blocking Zero VOC formula. It creates a uniform surface finish for improved hiding, adhesion and flow and leveling of topcoats. Intended for drywall, wood, plaster, concrete, CMU, brick, vinyl and non-ferrous metals. This acrylic latex film is mildew resistant and also suitable for sizing walls to install wallcovering.

## BEHR® Interior/Exterior Bonding Primer, 432 is specifically formulated to bond to a variety of ‘tough-to-paint’ surfaces. Its advanced chemistry provides a sound anchor for topcoats while reducing or potentially eliminating the need for sanding dense and glossy surfaces. This product may be used under epoxies, lacquers, products containing xylene or other hot solvents.

## BEHR® Interior/Exterior Metal Primer 435 is a rust-inhibitive primer that can be applied over clean and sound rusty metal surfaces while preventing corrosion with minimal surface preparation. This innovative water-based primer features fast dry time, low odor and easy clean-up.

## BEHR® Multi-Surface Interior/Exterior Stain-Blocking Primer & Sealer, 436 blocks medium to heavy stains and has excellent adhesion to multiple substrates. It offers corrosion and rust resistant properties to ferrous and non-ferrous metals. This low VOC product also provides a high-hide, mildew-resistant primer film with quick recoat time and can be applied to masonry surfaces with a pH level up to 13.

## BEHR Acrylic-Alkyd Enamel Undercoater 437 is a Low VOC water-based, alkyd primer that has excellent tannin stain-blocking and outstanding flow and leveling for wood. It provides great sandability and is designed for use under higher sheen paints on interior and exterior surfaces. This high-hide product also offers corrosion and rust resistant properties to properly prepared ferrous metal.

## BEHR PREMIUM® Concrete & Masonry Bonding Primer 880 is a high performance, water-based prep product designed specially to promote optimum adhesion to interior and exterior concrete and masonry surfaces.

## BEHR PRO® Block Filler Primer PR50 is an interior / exterior latex low VOC primer formulated to fill and seal porous masonry
surfaces, reduce pinholing and help produce a smooth and even topcoat for a uniform, professional quality finish.

## GENERAL SURFACE PREPARATION

Clean surfaces to receive paint thoroughly of substances, which could impair adhesion of paints, including dust, dirt, oil, grease and other contaminants before application of any coatings and stains. Prepare surfaces as follows:

WOOD: Remove mill glaze and dust, sand smooth. Fill open joints, cracks, nail holes and other pits or depressions flush and smooth with wood filler after priming. Use wood putty to match finish paint coat. Touch up knots or sap streaks with a stain-blocking sealer before priming. Prime exterior and interior woods with a water-based, stain-blocking primer.

### LAMINATE AND FIBERGLASS REINFORCED PLASTIC (FRP)

Remove grease, oil and dirt to achieve a clean, dry and slightly roughened surface before priming with a water-based bonding primer to increase proper adhesion.

CONCRETE, PRECAST CONCRETE and CONCRETE TILT-UP: Remove release agents, curing compounds, loose particles, efflorescence, and chalk. Do not coat surfaces if moisture content or alkalinity of surface to be coated exceeds that permitted in the manufacturer’s written instructions. Prime with a water-based alkali-resistant primer.

PLASTER and STUCCO: Fill hairline cracks, small holes, and imperfections on surfaces with patching compound. Smooth off to match adjacent surfaces. Rinse plaster and stucco with fresh water to neutralize high alkaline surfaces where they occur. Apply a water-based, stain-blocking, alkali-resistant primer.

MASONRY: Remove efflorescence and chalk. Do not coat surfaces if moisture content or alkalinity of surface  to be coated exceeds that permitted in the manufacturer’s written instructions. Prime with an alkali-resistant masonry primer.

SHOP-PRIMED STEEL: Solvent clean according to SSPC-SP1. Remove loose primer and rust, contaminants, and foreign matter. Prime bare steel and touch up abrasions with a ferrous metal primer.

STEEL, FERROUS METAL: Remove rust, mill scale, foreign substances, and shop primer. Clean according to SSPC-SP3, “Power Tool Cleaning”, or abrasive blasting cleaning according to SSPC-SP6 “Commercial Blast Cleaning” as required. Apply a stripe coat of primer to edges, welds, fasteners, and other irregular areas. Protect surface from corrosion until application of water-based, rust-inhibitive metal primer, recommended at the completion of surface preparation.

GALVANIZED METAL: Remove oils, passivators and clean entire surface with an appropriate solvent. Pre-treat with a phosphoric acid etching solution to promote adhesion of subsequently applied coatings. Prime with a water-based galvanized metal primer.

PHOSPHATIZED METAL or GALVANNEALED METAL shall not be chemically etched. Clean to remove grease, oil and dirt. Apply a water-based rust-inhibitive metal primer.

ALUMINUM: Solvent clean according to SSPC-SP1. Remove loose surface oxidation. Prime with a water-based bonding primer intended for aluminum.

GYPSUM BOARD: Remove dust and foreign matter. Fill pits flush and smooth with joint compound and where required, apply skim coat to provide the required Level of Finish. Apply suitable patching compound to repair gauges, holes, and voids. Sand smooth and clean to a dust free surface.

WARNING! If you scrape, sand, or remove old paint, you may release lead dust. Lead is toxic. Exposure to lead dust can cause serious illness, such as brain damage, especially in children. Pregnant women should also avoid exposure. Wear a NIOSH-approved respirator to control lead exposure. Clean up carefully with a HEPA vacuum and a wet mop. Before you start, find out how to protect yourself and your family by contacting the National Lead Information Center at 1-800-424-LEAD or log on to www.epa.gov/lead.

## PROJECT CONDITIONS FOR PAINTING EXTERIOR SURFACES

Do not apply paint or coatings when temperature is below 50ºF (unless otherwise noted). Do not apply exterior paint in damp or rainy weather; ensure that the surface has dried thoroughly before proceeding. Surface temperature must be at least 5°F above dew point before painting.

# INTERIOR PAINT SCHEDULE (09 91 23 INTERIOR PAINTING)

## ADMISSIONS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Satin Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Satin Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Satin Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR Premium Plus® Interior Semi-Gloss Enamel (3050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Galvanized-Metal: Aluminum, and Miscellaneous Non-Ferrous Metals

Light Industrial Coating: Low Odor/ VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Anodized Aluminum:

Light Industrial Coating: Low Odor/ VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432))

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## RECEPTION, WAITING AREAS, LOBBIES, AND COMMON AREAS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/ Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Satin Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR Premium Plus® Interior/Exterior Hi-Gloss Enamel (2-8050)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light   Industrial  Coating:

### Semi-Gloss Finish

Primer:    	BEHR® Interior/Exterior Metal Primer (435)

Two  Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## OFFICES, CONFERENCE ROOMS AND MULTI-PURPOSE ROOMS

### Gypsum Board: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre- Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

## HALLWAYS, CORRIDORS AND COMMON AREAS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Satin Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish:

### Primer:	BEHR® Interior/Exterior Metal Primer (435)

### Two: Coats:	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Galvanized-Metal: Aluminum, and Miscellaneous Non-Ferrous Metals

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

## NURSES’ STATION, ADMINISTRATIVE CENTER

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR Premium Plus® Interior/Exterior Hi-Gloss Enamel (2-8050)

Latex, Institutional, Low Odor/Zero VOC:

Satin Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel (7050)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR Premium Plus® Interior Semi-Gloss Enamel (3050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

### Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## EXAMINATION, CONSULTING AND TREATMENT ROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Satin Finish:

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR Premium Plus® Interior Satin Enamel, (2050)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## MEDICAL / CLINICAL PATHOLOGY AND LABORATORIES, LAB

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board – Ceilings

### Latex Institutional, Low Odor/Zero ZOC

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer:	BEHR PREMIUM PLUS® Interior Drywall Primer & Sealer (73)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss Enamel (HP150)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Galvanized-Metal: Aluminum, and Miscellaneous Non-Ferrous Metals

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### Anodized Aluminum

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## IMAGING / RADIOLOGY

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## PATIENT ROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Gypsum Board: Inpatient Bathroom, Toilet Walls and Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats: 	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete: Inpatient Bathroom Wet Areas

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete and Pre-Cast Concrete: Inpatient Bathroom, Toilet Walls and Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats: 	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete – Inpatient Bathroom Wet Areas

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Inpatient Bathroom, Toilet Walls and Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer	BEHR PRO® Block Filler Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish - High Performance Architectural

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats: 	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Inpatient Bathroom Wet Areas

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Semi-Gloss

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Metal Anodized Aluminum:

### Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## LABOR AND DELIVERY, RECOVERY AND MATERNITY SUITES

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Galvanized-Metal: Aluminum, and Miscellaneous Non-Ferrous Metals

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Anodized Aluminum:

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432))

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

## NURSERY

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Ferrous and Non-Ferrous Metal – Doors, Door Frames, Miscellaneous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Galvanized-Metal: Aluminum, and Miscellaneous Non-Ferrous Metals

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### Anodized Aluminum:

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432))

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## EMERGENCY ROOM, ER , ED

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## INTENSIVE CARE UNIT, ICU, SICU, AND SUBICU

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## NEONATAL INTENSIVE CARE UNIT, NICU

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

Anodized Aluminum:

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432))

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## OPERATING  ROOMS, OR - SURGICAL  SUITES,  MEDICAL/SURGICAL  UNITS,  MED SURGERY UNITS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Gypsum Board: Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Eggshell Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light   Industrial  Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:    	BEHR® Interior/Exterior Metal Primer (435)

Two  Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## PATIENT RECOVERY ROOMS, POST-OP

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board – Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## PATIENT REHABILITATION AND THERAPY ROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board and Plaster: Walls (Wet Areas)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

Anodized Aluminum:

Light Industrial Coating: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432))

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Pre-Treatment: Klean Strip Phosphoric Prep & Etch, (GKPA30220)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## PHARMACY

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## KITCHEN, FOOD PREPARATION AND FOOD SERVICES

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Walls and Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Gypsum Board: Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Walls and Wet Areas:

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150) Low Odor/VOC

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Walls and Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Walls and Wet Areas:

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

Latex, Institutional, Low Odor/VOC:

### Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR Premium Plus® Interior/Exterior Hi-Gloss Enamel (2-8050)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Gloss Paint (8200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

## CAFETERIA, RESTAURANT AND CAFÉ

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted, Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

### Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## MEDICAL STAFF LOUNGE, BREAKROOMS, STORAGE LOCKERS, TOILET ROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Extra Durable Flat Paint (1720)

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Ferrous and Non-Ferrous Metal – Doors, Door Frames, Miscellaneous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## LINEN  AND  LAUNDRY  SERVICES  (INCLUDING  WET  AREAS)

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Gypsum Board: Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## CENTRAL STERILE SERVICES, CSSD (Including Wet Areas)

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats: 	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas:

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Eggshell (HP140)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: (Wet Areas): Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## CENTRAL  SUPPLY  ROOM

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## JANITORIAL OFFICE, BREAK ROOM AND COMMON SPACE

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## CUSTODIAN ROOMS, JANITORIAL CLOSETS, STORAGE AND UTILITY ROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas:

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas:

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Wet Areas: Low Odor/VOC

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## PUBLIC RESTROOMS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC (Wet Areas)

### Semi-Gloss Finish

Primer: 	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Gypsum Board: Ceilings

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC (Wet Areas)

### Semi-Gloss Finish

Primer: 	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC (Wet Areas)

### Semi-Gloss Finish

Primer: 	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC (Wet Areas)

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Laminate and Fiberglass Reinforced Plastic (FRP)

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior /Exterior Bonding Primer (432)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne: Low Odor/VOC (Wet Areas)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Bonding Primer (432)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Light Industrial Coating: Low Odor/VOC

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### High Performance, Epoxy, Pre-Catalyzed, Waterborne:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR PRO® Pre-Catalyzed Waterborne Epoxy Semi-Gloss (HP150)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## ENGINEERING AND FACILITIES OFFICES, STORAGE ROOMS AND COMMON AREAS

### Gypsum Board and Plaster: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Gypsum Board: Ceilings

Latex, Institutional, Low Odor/Zero VOC:

### Flat Finish

Primer:	BEHR® Drywall Plus Interior Primer & Sealer (73)

Two Coats:	BEHR PRO® i300 Interior Dead Flat Paint (PR310)

### Concrete and Pre-Cast Concrete: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR® Interior Stain-Blocking Primer & Sealer (75)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Concrete Masonry Units CMU: Walls

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Eggshell Finish (virucidal and antibacterial paint)

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR® Copper Force™ Interior Eggshell Enamel (2190)

Latex, High Performance Architectural, Low Odor/VOC:

### Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Eggshell Enamel (2750)

Latex, Institutional, Low Odor/Zero VOC:

Eggshell Finish

Primer:	BEHR PRO® Block Filler and Primer (PR050)

Two Coats:	BEHR PRO® i300 Interior Eggshell Paint (PR330)

### Wood Opaque: Pre-Primed and Painted Doors, Door Frames, Trim, Base, and Woodwork

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, High Performance Architectural, Low Odor/VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR ULTRA Scuff Defense® Interior Semi-Gloss Enamel (3750)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Acrylic-Alkyd Enamel Undercoater (437)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

### Steel and Iron Metal: Doors, Door Frames, Cabinets, Piping, and Miscellaneous Ferrous Metal

Latex, Anti-Viral/Anti-Bacterial, Low Odor/Zero VOC:

### Semi-Gloss Finish (virucidal and antibacterial paint)

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR® Copper Force™ Interior Semi-Gloss Enamel (3190)

Latex, Institutional, Low Odor/Zero VOC:

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats:	BEHR PRO® i300 Interior Semi-Gloss Paint (PR370)

## WOOD – INTERIOR STAINED AND TRANSPARENT FINISHES

### Wood: Water-Based Polyurethane over Water-Based Stain

Stain Coat:	BEHR® Fast Drying Water – Based Wood Stain (B4500)

Three Coats:	BEHR® Fast Drying Water – Based Polyurethane

- BEHR® Fast Drying Water-Based Polyurethane Matte (B8106)

- BEHR® Fast Drying Water-Based Polyurethane Satin (B8100)

- BEHR® Fast Drying Water-Based Polyurethane Semi-Gloss (B8102)

- BEHR® Fast Drying Water-Based Polyurethane Semi-Gloss (B8104)

## WOOD – INTERIOR CLEAR TRANSPARENT FINISHES

### Wood: Water-Based Polyurethane over Water-Based Stain

Three Coats:	BEHR® Fast Drying Water – Based Polyurethane

- BEHR® Fast Drying Water-Based Polyurethane Matte (B8106)

- BEHR® Fast Drying Water-Based Polyurethane Satin (B8100)

- BEHR® Fast Drying Water-Based Polyurethane Semi-Gloss (B8102)

- BEHR® Fast Drying Water-Based Polyurethane Semi-Gloss (B8104)

## CONCRETE FLOORS – PAINTED PEDESTRIAN TRAFFIC

### Concrete, New or Previously Painted Surfaces

Water-Based, Low VOC Coating:

### Anti-Slip Texture, Low-Lustre  Finish

Primer:	BEHR® Concrete & Masonry Bonding Primer (880)

Two Coats: 	BEHR PREMIUM® Anti-Slip Texture Low-Lustre Enamel Porch & Patio Floor Paint (6250)

Water-Based, Low VOC Coating:

### Low-Lustre  Finish

Primer:	BEHR® Concrete & Masonry Bonding Primer (880)

Two Coats: 	BEHR PREMIUM® Low-Lustre Enamel Porch & Patio Floor Paint (6050)

## CONCRETE FLOORS – PAINTED, HEAVY TRAFFIC (Behr Paint is an Authorized Distributor of Monopole, Inc.)

### Concrete – Previously Painted

Water-Based, Catalyzed Aliphatic Polyurethane Coating:

### Matte Finish

Primer:	Monochem Monobond Multi-Surface Primer, Sealer & Bonder (1990)

Two Coats:	Monochem Permashield® 200 2K Water-Based Aliphatic Polyurethane (5365)

### Concrete – New

Water-Based, Catalyzed Aliphatic Polyurethane Coating:

### Matte Finish

Primer:	Monochem 21 Epoxy Primer (2121)

Two Coats:	Monochem Permashield® 200 2K Water-Based Aliphatic Polyurethane (5365)

# EXTERIOR PAINT SCHEDULE (09 91 13 EXTERIOR PAINTING)

## CONCRETE

### Precast, Poured in Place, Tilt-Up Concrete: Walls

### Latex, Acrylic System

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Flat Paint (PR610)

### Satin Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Satin Paint (PR640)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Semi-Gloss Paint (PR670)

Latex, Acrylic High Build Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PREMIUM® Exterior High Build Coating (4700)

Texture-Medium, Acrylic Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® Exterior Acrylic Texture Coating - Medium (PR710)

## STUCCO  AND  CEMENT PLASTER

### Stucco, EIFS and Cement Plaster – Walls

### Latex, Acrylic System

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Flat Paint (PR610)

### Satin Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Satin Paint (PR640)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Semi-Gloss Paint (PR670)

Latex, Acrylic High Build Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PREMIUM® Exterior High Build Coating (4700)

Texture-Medium, Acrylic Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® Exterior Acrylic Texture Coating - Medium (PR710)

## FIBER CEMENT: PRE-PRIMED

### Fiber Cement – Walls

### Latex, Acrylic System

### Flat Finish

Spot Prime:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Flat Paint (PR610)

### Satin Finish

Spot Prime:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Satin Paint (PR640)

### Semi-Gloss Finish

Spot Prime:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Semi-Gloss Paint (PR670)

Texture-Medium, Acrylic Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® Exterior Acrylic Texture Coating - Medium (PR710)

## CONCRETE MASONRY UNITS (CMU)

### Concrete Block and Cinder Block – Walls

### Latex, Acrylic System

### Flat Finish

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats: 	BEHR PRO® e600 Exterior Flat Paint (PR610)

### Satin Finish

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats: 	BEHR PRO® e600 Exterior Satin Paint (PR640)

### Semi-Gloss Finish

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats: 	BEHR PRO® e600 Exterior Semi-Gloss Paint (PR670)

Latex, Acrylic High Build Coating

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PREMIUM® Exterior High Build Coating (4700)

Texture-Medium, Acrylic Coating

### Flat Finish

Primer:	BEHR PRO® Block Filler Primer (PR050)

Two Coats: 	BEHR PRO® Exterior Acrylic Texture Coating - Medium (PR710)

## CONCRETE, UNFINISHED DECKS, STONE, AND BRICK

### Exterior Concrete – Horizontal and Vertical Surfaces

### Clear, Water-Based Sealer and Waterproofer:

Primer:	BEHR PREMIUM® Concrete & Masonry Protector & Waterproofer (980)

Two Coats: 	BEHR PREMIUM® Concrete & Masonry Protector & Waterproofer (980)

## WOOD – PAINTED

### Wood and Wood Composites – Painted

### Latex, Acrylic System

### Flat Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Flat Paint (PR610)

### Satin Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Satin Paint (PR640)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR PRO® e600 Exterior Semi-Gloss Paint (PR670)

Gloss Finish

Primer:	BEHR® Interior/Exterior Multi-Surface Primer & Sealer (436)

Two Coats: 	BEHR Premium Plus® Hi-Gloss Enamel Paint (8050) (2-8050 SCAQMD))

## WOOD: STAINED, WATERPROOFING STAINS

### Wood and Wood Composites – Stained

### Solid Color Finish

Stain Coat:	BEHR PREMIUM® Solid Color Waterproofing Stain & Sealer (5011)

### Wood, Engineered Synthetic Wood, and Pressure Treated Lumber – Stained

### Semi-Transparent Finish

Stain Coat:	BEHR PREMIUM® Semi-Transparent Waterproofing Stain & Sealer (5077)

## WOOD: EXTERIOR TRANSPARENT FINISHES

### Wood Clear Finish:

### Exterior Spar Urethane, Water-Based: (Not recommended for use on exterior wood siding, decks and stairs.)

Three Coats:	BEHR® Water-Based Spar Urethane

- Behr® Water-Based Spar Urethane Satin (B8200)

- Behr® Water-Based Spar Urethane Semi-Gloss, (B8202)

- Behr® Water-Based Spar Urethane, Gloss, (B8204)

## FERROUS METAL: STEEL AND WROUGHT IRON

### Light Industrial Coating Systems

### Eggshell Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### Gloss Finish

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Gloss Paint (8200)

## NON-FERROUS METAL: GALVANIZED STEEL

### Light Industrial Coating

### Eggshell Finish

Pretreatment:	Klean Strip Phosphoric Prep & Etch GKPA30220

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish

Primer:		BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 		BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### Gloss Finish

Primer:		BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 		BEHR® Interior/Exterior Direct-To-Metal Gloss Paint (8200)

## ALUMINUM

### Light Industrial Coating

### Eggshell Finish

Pretreatment:	Klean Strip Phosphoric Prep & Etch GKPA30220

Primer:	BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 	BEHR® Interior/Exterior Direct-To-Metal Eggshell Paint (7200)

### Semi-Gloss Finish – Light Industrial Coating

Primer:		BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 		BEHR® Interior/Exterior Direct-To-Metal Semi-Gloss Paint (3200)

### Gloss Finish – Light Industrial Coating

Primer:		BEHR® Interior/Exterior Metal Primer (435)

Two Coats: 		BEHR® Interior/Exterior Direct-To-Metal Gloss Paint (8200)